# Text boxes

Project 1

5/3/2016 2:04:14 PM

Comment:

Spectrum processing : Yellow TR

No peaks omitted

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 58.18 | 79.16 |  |
| O K | 8.87 | 9.06 |  |
| Na K | 3.76 | 2.67 |  |
| Mg K | 0.22 | 0.15 |  |
| Si K | 0.81 | 0.47 |  |
| P K | 2.14 | 1.13 |  |
| Cl K | 1.98 | 0.91 |  |
| K K | 0.29 | 0.12 |  |
| Ca K | 0.95 | 0.39 |  |
| Fe K | 4.57 | 1.34 |  |
| Cu K | 17.76 | 4.57 |  |
| Au L | 0.47 | 0.04 |  |
| Totals | 100.00 |  |  |

Project 1

5/3/2016 2:34:06 PM

Comment:

Spectrum processing : Green

No peaks omitted

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 9.59 | 20.40 |  |
| O K | 13.39 | 21.39 |  |
| Na K | 26.67 | 29.64 |  |
| Si K | 1.00 | 0.91 |  |
| P K | 4.75 | 3.92 |  |
| S K | 0.64 | 0.51 |  |
| Cl K | 12.75 | 9.19 |  |
| K K | 0.96 | 0.63 |  |
| Ca K | 3.43 | 2.19 |  |
| Fe K | 10.29 | 4.71 |  |
| Cu K | 16.04 | 6.45 |  |
| Au L | 0.50 | 0.07 |  |
| Totals | 100.00 |  |  |

Project 1

5/3/2016 2:56:11 PM

Comment:

Spectrum processing : Pink

No peaks omitted

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 52.22 | 76.79 |  |
| O K | 10.25 | 11.32 |  |
| Si K | 0.29 | 0.18 |  |
| P K | 3.35 | 1.91 |  |
| K K | 0.34 | 0.16 |  |
| Ca K | 0.61 | 0.27 |  |
| Fe K | 6.31 | 2.00 |  |
| Cu K | 26.50 | 7.37 |  |
| Au L | 0.12 | 0.01 |  |
| Totals | 100.00 |  |  |

Project 1

5/3/2016 3:15:54 PM

Comment:

Spectrum processing :  Red

No peaks omitted

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 36.75 | 58.91 |  |
| O K | 16.56 | 19.94 |  |
| Na K | 6.81 | 5.71 |  |
| Si K | 0.25 | 0.17 |  |
| P K | 5.25 | 3.26 |  |
| Cl K | 3.42 | 1.86 |  |
| K K | 0.90 | 0.44 |  |
| Ca K | 1.07 | 0.52 |  |
| Fe K | 10.73 | 3.70 |  |
| Cu K | 18.10 | 5.49 |  |
| Au L | 0.16 | 0.02 |  |
| Totals | 100.00 |  |  |

Project 1

5/3/2016 3:36:01 PM

Comment:

Spectrum processing :  Orange TR

Peak possibly omitted : 4.518 keV

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 9.94 | 24.95 |  |
| O K | 15.07 | 28.39 |  |
| Na K | 1.85 | 2.42 |  |
| Si K | 0.37 | 0.40 |  |
| P K | 13.06 | 12.71 |  |
| Cl K | 1.07 | 0.91 |  |
| K K | 0.86 | 0.66 |  |
| Ca K | 0.84 | 0.63 |  |
| Fe K | 30.21 | 16.30 |  |
| Cu K | 26.59 | 12.61 |  |
| Au L | 0.13 | 0.02 |  |
| Totals | 100.00 |  |  |

Project 1

5/3/2016 3:58:23 PM

Comment:

Spectrum processing :  Blure TR

Peak possibly omitted : 4.038 keV

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 15.46 | 32.96 |  |
| O K | 21.34 | 34.16 |  |
| Na K | 2.48 | 2.77 |  |
| Si K | 0.26 | 0.24 |  |
| P K | 8.78 | 7.26 |  |
| Cl K | 0.75 | 0.54 |  |
| K K | 2.86 | 1.87 |  |
| Fe K | 17.63 | 8.08 |  |
| Cu K | 29.89 | 12.05 |  |
| Au L | 0.54 | 0.07 |  |
| Totals | 100.00 |  |  |

Project 1

5/3/2016 4:17:34 PM

Comment:

Spectrum processing :  Purple

No peaks omitted

Quantitation method : Cliff Lorimer thin ratio section.

Processing option : All elements analyzed (Normalised)

Number of iterations = 1

Standardless

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C K | 13.99 | 27.58 |  |
| O K | 25.17 | 37.26 |  |
| Na K | 7.85 | 8.09 |  |
| Si K | 0.60 | 0.51 |  |
| P K | 13.00 | 9.94 |  |
| Cl K | 1.92 | 1.29 |  |
| K K | 0.86 | 0.52 |  |
| Ca K | 0.67 | 0.40 |  |
| Fe K | 19.93 | 8.45 |  |
| Cu K | 15.99 | 5.96 |  |
| Au L | 0.02 | 0.00 |  |
| Totals | 100.00 |  |  |